# Technical Data Sheet                  RED DEVIL, INC.

Product:		Lifetime Siliconized Acrylic - Clear

Product No.:		#0866 Series (0865, 0866, 0869)

Description:  Lifetime Siliconized Acrylic Clear, is formulated with silicone for applications where a high quality clear seal is desired. This multi-purpose sealant is paintable and can be used for a variety of applications but should be protected from water until cured. Product applies white and dries clear in 2 weeks or less, depending on temperature, humidity and bead size.

Performance Specs: ASTM C834-00 Type C

Typical Properties:

Extrusion-viscosity			7 ± 2 seconds (Semco @ 50 psi)

Weight per gallon			9.0 ± 0.50 lbs.

% Solids (TNV)				62.5 ± 2.5

pH						8.5 ± 0.5

Color					White (Initially),	 Ultra Clear (Cured)

Odor					Mild Acrylic

Shrinkage				Less than 50%

Application Temperature Range			40F to 90F (5C to 32C)

Tack-free Time				2 Hours

Full Cure				72 Hours (Full clarity is reached in 3 - 14 days.)

Paint Over Time				After full clarity is reached.

Flash Point				Greater than 200F (94C)

Freeze/Thaw Stability			Passes 5 cycles

Stain Resistance				Excellent

Slump Resistance			Excellent

Water Resistance			Excellent (when cured)

Crack Resistance			Excellent (when cured)

Durability/Weathering			Excellent - No cracking @ 5,000 hrs. in weather tester

Percent Elongation at Break			1000 ± 100

25% Extension/Recovery			98% ± 1

Tensile Strength at Break			<10 psi

Flexibility				Passes 1", 2" and 4" Mandrell bend @ 40 F

Clean-up Solvent (before cure)			Water

Coverage				50 - 55 linear feet (3/16" bead) (cartridge)

Service Temperature Range			0F to 200F (-18C to 94C)

Shelf Life				1 year unopened @ 77F (25C)

Storage				Store at temperatures above freezing.

Standard Container			HDPE cartridge & squeeze tube

VOC:                                                           64.6 g/L

CARB Compliance:                                        YES

Prop 65 Ingredients:                                      NONE

Recommendations for use of this product are based on tests we believe to be reliable.  Manufacturer and seller are not responsible for results where this product is used under conditions beyond our control.  Under no circumstances will Red Devil, Inc. or the seller be liable to anyone in excess of the purchase price of this product.                                                                    Issue Date: July 9, 2002